MasterSpec (a product of the AIA)

- 104513 - Photoluminescent Egress Path Markings.

MasterFormat (CSI)

- 104500 - Photoluminescent Exit Specialties.

Form-A-Tread® GLOW™

PRODUCTS

SUMMARY

Section includes a proprietary photoluminescent form-in-place, anti-slip, epoxy compound for use as an anti-slip component in conjunction or in lieu to the sections listed above.

SUBMITTALS

Product Data: For each type of product required on Project.

Samples: Submit one 12-inch-long sample of each selected color, width and finish required on Project. Sample shall be submitted to Architect on types of concrete, metal and wood, required for the project.

MOCKUP

Construct mockup illustrating design or pattern intent including all materials to be used in actual Project. Provide exposed material in exact color and texture as selected from Samples.

Locate [where directed by Architect.] [where indicated on Drawings.]

Incorporate accepted mockup as part of Work.

****** [OR] ******

Remove mockup [when directed by Architect.] [________.]

FIELD CONDITIONS

Environmental Limitations: Comply with manufacturer's written instructions for substrate temperature, ambient temperature, moisture, ventilation, and other conditions affecting epoxy tread system installation.

Close spaces to traffic during epoxy tread system installation and for not less than 6 hours after installation unless manufacturer recommends a longer period.

PRODUCTS

PERFORMANCE

Form- A-Tread GLOW is 2015 ICC IBC and 2014 NYC Construction Code BC 1024.4 Compliant and meets or exceeds the requirements of ASTM E 2072

PHOTOLUMINESCENT, SLIP RESISTANT, FORM-IN-PLACE EPOXY TREAD SYSTEM

Manufacturer (Proprietary; US Patent 10,577,475):

Form-A-Tread Company div. of RGF Materials Company (LLC)

Product Description: A single coat, fast curing, photoluminescent and slip resistant 100% epoxy formula designed to create permanent, slip resistant and luminous egress path marking on the horizontal leading edge of steps and landings. [Form-A-Tread GLOW][Epoxy-based photoluminescent tread making material] is applied in 1 coat and adheres to porous and non-porous surfaces including concrete, stone, brick, wood, fiberglass, and metal with no priming of substrate required.   [Form-A-Tread GLOW][Epoxy-based photoluminescent tread making material] is ready to receive traffic in less than 6 hours and is exceptionally durable in areas exposed to heavy pedestrian traffic, temperature extremes, and chemical exposure.

Thickness:  1 coat applied to 30 mils minimum using patent pending EZ Form taping stencil or Form Tape supplied by Manufacturer.

Width: [As selected by Architect.][As indicated on Drawings.]

Color: Greenish White / Glow-in-the-Dark.

Broadcast Material: [As selected by Architect from manufacturer’s full range][Consult manufacturer for applicable options.]

COMPONENTS

Dual component cartridge with Mix Nozzle.

ACCESSORIES

EZ Form®, Form Tape, Spreader and Dispensing Tool.

EXECUTION

EXAMINATION

Verify surface is free of foreign matter and surface is clean, dry and sound in accordance with manufactures recommendations.

PREPARATION

Prepare existing surface in accordance with manufactures recommendations.

INSTALLATION

Apply formed-in-place epoxy system in approved width, depth, spacing and length acceptable to Architect and as indicated on Drawings.  Apply system in spacing acceptable to Architect and as indicated Drawings.

CLEANING

Clean-up excess epoxy system in accordance with manufactures recommendations.

PROTECTION OF FINISHED WORK

Do not permit traffic over formed-in-place epoxy system for a minimum of 6 hours.

END OF FORM-A-TREAD GLOW